## Slide 1
Presenters:
Fyodor Morozko
Roza Navitskaya

## Slide 2: Outline
Introduction
Design of nanophotonic structures
Inverse design problem
Tandem neural network
Design of 1D multilayer structures
Design of 2D structures
Conclusion

## Slide 3: Design of Nanophotonic Structures
Approaches in nanophotonic structures design:
Conventional: iteratively performed optimization (evolutionary algorithms, level set methods, adjoint methods, optimization of specific geometric parameters)
  straightforward methods based on electromagnetic simulations
  computationally expensive and slow, as each design requires a large amount of simulations
Data-driven: based on machine learning techniques (NNs are trained to assist in the design process)
  a large amount of training instances is needed, which requires significant amounts of computational resources
  greatly reduced design time, as simulations are performed only once before training the NN
  inverse design problem can lead to bad convergence of the NN

## Slide 4: Design of Nanophotonic Structures
NNs can be used in two different ways:
(a) Forward-modeling networks: take the input of the structural parameter D (such as the geometrical shape of a nanostructure) and predict the electromagnetic response R of the device.
(b) Inverse-design networks: take the EM response R as the input and directly output the structure D.

## Slide 5: Design of Nanophotonic Structures
Design:
The goal is to generate a target transmission spectrum using a multilayer film consisting of alternating layers of SiO2 and Si3 N4.
The design space is the thickness of each layer.

## Slide 6: Inverse Design Problem
Inverse Design Problem:
The same EM response R can be created by many different designs D. This nonunique response-to-design mapping creates conflicting training instances, such as (R, DA) and (R, DB).
When such conflicting instances with the same input but different output labels exist in the training data set, the neural network would be hard to converge.

## Slide 7: Inverse Design Problem
Example of an inverse-design network training:
Training is done by minimizing a cost function: , where is the layer thickness designed by the neural network given the input R, and is the ground truth of the layer thickness.
The fully-connected NN had 4 layers with number of weights 200−500−200−20.
Training set: 500 000 instances, test set: 50000 instances.
Nonunique instances are eliminated (filtered data)
Nonunique instances are present (unfiltered data)

## Slide 8: Inverse Design Problem
Possible solution (ineffective):
Divide the training data set into distinct groups, so that within each group there is unique design D corresponding to each response R.
However, there may be implicit conflicting instances in the dataset. For example, let and be self-consistent datasets generated using operators and that satisfy and . When and are combined to generate a new dataset , the dataset is not self-consistent.

## Slide 9: Inverse Design Problem
Proposed solution:
Use a tandem network. By cascading an inverse-design network with a forward-modeling network, the tandem network can be trained effectively.
A desired response R is taken as the input. The output by the intermediate layer M is the designed structure D. The output of the tandem network is the response calculated from the designed structure.
The forward modeling network is trained in advance. Then, the weights in the pretrained forward modeling network are fixed and the weights in the inverse network are adjusted to reduce the cost.

## Slide 10: Tandem Neural Network
Proposed solution:
This network structure overcomes the issue of nonuniqueness in the inverse scattering of electromagnetic waves because the design by the neural network is not required to be the same as the real design in training samples.
Instead, the cost function would be low as long as the generated design and the real design have similar response.

## Slide 11: Tandem Neural Network
Training a tandem network:
The inverse network architecture is set to have four layers with each layer having 200−500−200−20 units.

## Slide 12: Tandem Neural Network
Training a forward-modeling network:
The number of hidden layers and weights in them can be varied.
Architecture 1: 20 − 500 − 200
Architecture 2: 20 − 500 − 200 − 200
Architecture 3: 20 − 500 − 200 − 200 − 200
Architecture 4: 20 − 500 − 200 − 200 − 200 − 200
Architecture 4: 20 − 500 − 200 − 200 − 200 − 200
Architecture 5: 20 − 500 − 500 − 200 − 200 − 200
Architecture 6: 20 − 500 − 500 − 500 − 200 − 200

## Slide 13: Design of 1D Multilayer Structures
Design of 1D multilayer structures:
Designing the structure of 16-layer SiO2 and Si3N4 thin film for target transmission spectra of a Gaussian shape:
The maximum thickness of each layer is set to be 150 nm. The response is the transmission spectrum within the range of 300 to 750 THz.

## Slide 14: Design of 2D Structures
Design of 2D structures:
Designing 2D structures to modulate transmission phase delay independently at three wavelengths: R (470 nm), G (540 nm), B (667.5 nm).
The designed units are composed of 3 layers of Si and SiO2. Within each layer, part of Si or SiO2 is removed to form a rectangular slot. The design parameters are thicknesses of the 3 layers di (i = 1, 2, 3), the location xi and width wi of the vacuum slot in the ith layer (i = 1, 2, 3).
This meta unit can be used in a metasurface to create three-color holograms.

## Slide 15: Design of 2D Structures
Design of 2D structures:
The training data set includes 750 000 instances and test data set includes 5000 instances.
The phase delay of the designed structure has an average error of 16.0°.

## Slide 16: Design of 2D Structures
Design of 2D structures:
The forward modeling neural network has 6 hidden layers with each layer having 1024 – 512 – 512 – 256 – 256 – 128 hidden units.
The inverse design network has 2 hidden layers with 512 and 256 hidden units.

## Slide 17: Conclusion
Shown that using neural networks for the inverse design suffers from the problem of nonuniqueness, a typical issue in the inverse scattering problem.
This issue makes it very difficult to train neural networks on a large training data set, which is often needed to model complex photonic structures.
Demonstrated a tandem architecture that tolerates both explicit and implicit nonunique training instances. It provides a way to train large neural networks for the inverse design of complex photonic structures.